## Slide 1
Spring 2017

## Slide 2: Nuclear fuel depletion calculations with Origen

## Slide 3: How do we calculate used fuel isotopic content?
Origen (part of SCALE) is used to calculate isotopic inventories for an assembly, given:
  A collapsed one-group cross-section library
  Fuel assembly initial enrichment
  Assembly irradiation history & cooling time

## Slide 4: Origen libraries are pre-calculated lattice physics solutions
Origen solves for the time-dependent neutron flux in the assembly using lattice physics transport tools like TRITON
Calculating an “assembly average” flux and collapsing to one group, this time-dependent flux is then used to solve for isotopic concentrations
Notes: ORIGEN works off of collapsed, one-group assembly-average cross-sections, representing a reaction rate within an assembly to solve for isotopic concentrations by solving the Bateman Equations / transition matrix. Because spectrum shape changes with irradiation, ORIGEN uses interpolated cross-sections to the nearest burnup / composition value.
Note that a one-group calculation is okay; it still preserves the reaction rate, which is what is important!

## Slide 5: What do ORIGEN calculations assume?
“Assembly-averaged” burnup characteristics – i.e., flux, burnup, etc. produces “averaged” isotopic concentrations
  Works well for “bulk” assembly characteristics – i.e., decay heat, concentrations, etc.
In other words, an “average,” uniform burnup across the assembly – point depletion

## Slide 6: Origen depletion calculation flow
OPUS
Origen reactor data libraries
Burnup
Enrichment
Origen
Cycle history
Initial compositions
Cycle powers [MW]
Irradiation times
Down / decay times
Cycle powers [MW/MTU]
Irradiation times
ARP
Problem-specific reactor data
Depleted material compositions
Formatted inventories / responses (e.g., decay heat, activity, radiotoxicity)

## Slide 7: Origen reactor data library interpolation
Interpolate
5% 235U
4% 235U
4.2% 235U
3% 235U

## Slide 8: ARP input format (LEU / UOX)
{ Configuration name }
{ enrichment [% U-235] }
{ # of cycles } { Fuel irradiation period(s) [days] }
{ Average cycle power [MW/MTU] }
{ # interpolations per cycle }
{ Moderator density [g/cm3] }
{ Interpolated library name }
e.g, w17x17
235U initial %
1 irradiation period per cycle
1 power (MW/MTU) per cycle
e.g.,: “w17_interpolated.f33”

## Slide 9: ARP input example (UOX)
=arp w17x17
3.65
3
400 400 350
40 35 30
1 1 1
0.732
w17_interpolated.f33
end
Westinghouse 17x17 lattice
3.65 % initial enrichment
3 irradiation cycles
40, 35, & 30 MW/MTU
Interpolated library name
400, 400, & 350 day cycle lengths
1 library per cycle
0.732 g/cm3 mod. density

## Slide 10: Origen input structure
Origen inputs are organized into cases
Each “case” block represents a single irradiation or decay cycle
  Typically, each irradiation cycle uses a new interpolated library position
    i.e., representing the nearest interpolated burnup
Material compositions can be passed from one case to the next

## Slide 11: SON syntax basics
Origen 6.2 uses SON (Standard Object Notation) syntax for input
[ arrays ]
Consist of one or more numbered entries in brackets
e.g., time=[ 10 20 30 … ]
{ blocks }
Contain keys and arrays within curly braces
e.g., case(caseLabel){ … }

## Slide 12: Array entry shortcuts
SON arrays allow for input shortcuts (similar to MCNP)
Repeat [R]
N R X
3 r 1E14 → 1E14 1E14 1E14
Linear interpolation [I]
N I X Y
3 i 5 1 → 5 4 3 2 1
Logarithmic interpolation [L]
N L X Y
5 L 1E-9 1E-3 → 1E-9 1E-8 1E-7 1E-6 1E-5 1E-4 1E-3

## Slide 13: Origen input structure
'SCALE comment
=origen
% ORIGEN comment
bounds{ … }
solver{ … }
options{ … }
case(A){
time=[31 365] % days
…
}
case(B){
…
}
% more cases?
end
Global problem configuration blocks
Each cycle (irradiation or decay) is a case block with time, powers, and (optionally) library & materials
Multiple cases can be chained together to represent an irradiation history
Notes: Note that the first case must specify a library; other cases use the library from the last case unless otherwise specified!

## Slide 14: Origen case block components
Cases consist of the following blocks:
case(label){
time{…} lib{…}
power=[…]
mat{…} print{…} save{…} neutron{…} gamma{…} beta{…}
alpha{…}
}
Specify which steps to save & output file (.f71)
Optional blocks to control output of gamma, neutron, alpha, and beta emissions
Control output print options
Specify problem materials
Problem powers (in MW)
Specify problem times & time units
Data library & position to use

## Slide 15: Specifying times with the time block
Times may be expressed one of two ways:
  Via a time array, i.e., time=[ … ]
    Default unit of days
  Via a time block (with units explicitly indicated)
    Available units: seconds, minutes, hours, days, and years
time{
t = [ 5 15 300 ]
units = HOURS
}
time=[ 5 15 300 ]
Array
Block

## Slide 16: Specifying start time with start=
By default, the start time begins where the last case left off
case{
mat{ … }
time=[ 1 10 25 50]
flux=[ 4r1e14 ]
}
% continuation case (time zero is 50 days)
case{
time{
units=YEARS
start=0
t=[0.1 0.3 0.9 2.7]
}
}
First case: end time is 50 days
Reset start time to 0 years
otherwise need to start at 50+365+0.1

## Slide 17: Library specification example
case{
mat{ … }
time=[ … ]
power=[ … ] lib{ file="w17_interp.f33"
pos=1
} % end lib
}
% continuation case (same library, new position)
case{
time=[ … ]
lib{ pos=2 }
}
Use 1st position on ARP-interpolated library
Use 2nd position on same interpolated library

## Slide 18: Specifying problem materials
=origen
case{
…
% create a material with 1 kg
% of 3% enriched LEU
mat{
units=GRAMS
iso=[u238=970.0E3 u235=3.0E4 o=123.1E3]
}
…
} % end case
end
Valid units include grams, gram-atoms / moles and curies
Specifying only elemental symbol uses natural abundances for each isotope
Can specify individual isotope masses as key/value pairs
Note: First case must always specify materials!

## Slide 19: Loading materials from a previous case
=origen
case(first) {
mat{
units=GRAMS
iso=[u238=970.0E3 u235=3.0E4 o=123.1E3]
}
…
} % end case
case(second) {
% load materials from step 4 of last case
mat{ previous=4 }
…
}
end
Load from step 4 of last case
(Default: previous=LAST)

## Slide 20: Loading materials from a saved file
=origen
case{
…
% Load from position 2 on saved f71 file
mat{
load{ file="origen_saved.f71" pos=2 }
} % end mat
…
} % end case
end

## Slide 21: Specifying irradiation powers: the power array
=origen
case{
…
mat{
units=GRAMS
iso=[u238=970.0E3 u235=3.0E4 o=123.1E3]
}
% 10 steps at 35 MW each
% 14,000 MWd/MTU total cycle burnup
powers=[ 10R 35.0 ]
times=[ 8I 10 400.0 ]
} % end case
end
Note: Powers are in total MW (not MW/MTU)
10 steps of all the same power (35 MW); can be different powers for each time interval
# times = # powers (Origen supplies t0 by default)

## Slide 22: Saving case outputs: the save block
=origen
case(rad){
…
} % end case
case(decay){
time{
start=0
t=[ 1 3 10 30 100 300 1000]
units=YEARS
}
save{
file="decay.f71"
steps=[ 0 3 7 ]
}
} % end case
end
Save concentrations to “decay.f71” for later analysis & restarts
Save concentrations at initial step (time 0), then at steps 3 (10 years) and 7 (1000 years)

## Slide 23: Other save options: LAST
=origen
…
case(decay){
time{
start=0
t=[ 1 3 10 30 100 300 1000]
units=YEARS
}
save{
file="decay.f71"
steps=[LAST]
}
} % end case
end
Save concentrations only for last time step (1000 years)

## Slide 24: Other save options: ALL
=origen
…
case(decay){
time{
start=0
t=[ 1 3 10 30 100 300 1000]
units=YEARS
}
save{
file="decay.f71"
steps=ALL
}
} % end case
end
Save concentrations for all time steps

## Slide 25: Origen print options
Origen output can be printed by nuclide [nuc] or by element [ele]
Output can be limited by nuclide library type
  Actinides [ac], fission products [fp], and light elements [le]
Origen supports output across a number of different units
  grams, moles / gram-atoms, decay heat, weight / atom %, radiotoxicity, etc.

## Slide 26: Origen output units (for decay cases)
Unit name | Description
GRAMS | Mass in grams
MOLES (or GRAM-ATOMS) | Number of moles of material
CURIES | Activity in Curies
BECQUERELS | Activity in Becquerels
ATOMS_PPM | Atom fractions (x 106)
WEIGHT_PPM | Weight fractions (x 106)
WATTS | Total decay heat (in watts)
G-WATTS | Total decay heat from photons (in watts)
M3_AIR | Radiotoxicity (in m3) for inhalation
M3_WATER | Radiotoxicity (in m3) for ingestion

## Slide 27: Origen output print examples
% print each nuclide (with totals across each sub-library) in grams
print{
nuc{ total=yes units=GRAMS }
}
% print each element (sub-library totals) in grams, moles, and curies
% Specify a minimum cutoff threshold of 1%
print{
ele{ total=yes units=[GRAMS MOLES CURIES] }
cutoffs[ ALL=1.0 ]
}
% print decay heat & mass (by element) ONLY for fission products & actinides
print{
ele{ sublibs=[AC FP] units=[GRAMS WATTS] }
}

## Slide 28: Origen sample problems

## Slide 29: 252Cf decay example: Decay for 10 years
=origen
bounds{ neutron=[ 20L 2.0E7 1.0E-5] }
case{
title="Cf-252 decay"
lib{ file="end7dec" pos=1 }
time{
units=YEARS
t=[ 0.01 0.03 0.1 0.3 1 3 10 ]
}
mat{
units=CURIES
iso=[cf252=1.0]
}
neutron=yes
}
end

## Slide 30: Simple depletion example
=origen
case(rad){
lib{ file="myInterpLib.f33" pos=1 }
time=[ 8I 10 300 ]
power=[ 10R 30.0 ]
mat{
units=GRAMS
iso=[u235=32.5E3 u238=967.5E3]
}
}
case(decay){
time{
t=[ 10L 1.0 10.0 ]
units=YEARS
}
save{
file="simple.f71"
steps=ALL
}
}
end
Irradiate 1 MT of 3.25% LEU for 300 days at 30 MW power
Decay for 10 years and save all decay steps
Notes: “

## Slide 31: Your turn: a simple irradiation case
Create an input to simulate one irradiation cycle of a Westinghouse 17x17 PWR assembly, (w17x17) with the following parameters:
  4.0% initial enrichment
  35 MW/MTU
  400 days irradiation
  30 days cooling time
  0.73 g/cm3 moderator density
  Assume 1 MTU (1E6 grams) starting mass
Make sure to save all decay steps

## Slide 32: Plotting Origen results in Fulcrum
In Fulcrum, open the saved .f71 file you created with your concentrations from your depletion case
In Fulcrum, select “watts” for plot units & sort units
  What nuclides dominate short-term decay heat?
Tip: Clicking on the “Table” tab at the top of the graph will give a tabular listing of nuclides for each time step

## Slide 33: Your turn: Extending your depletion case
Add two more irradiation and decay cases to your input
  Use the following powers:
    35 MW for the second cycle
    25 MW for the third cycle
  Each irradiation cycle should be 400 days
  The down time between cycles should be 30 days
  Track the decay after discharge for 10 hours post-discharge
Plot:
  The activity of 135Xe & 135I as a function of time. What happens after each discharge?
    Hint #1: Plot in hours
    Hint #2: Zoom in!

## Slide 34: MOX fuel calculations with Origen

## Slide 35: Introduction to MOX fuel calculations
Mixed-oxide (MOX) fuel calculations (U/Pu fuel) can be performed similarly to LEU/UOX calculations: only the ARP interpolation format changes

## Slide 36: ARP input format for MOX fuel
{ Configuration name }
{ Pu fraction [% Pu] }
{ Pu enrichment [% Pu-239 / Pu] }
{ dummy entry – e.g., 1.0 }
{ # of cycles }
{ Fuel irradiation period(s) [days] }
{ Average cycle power [MW/MTU] }
{ # interpolations per cycle }
{ Moderator density [g/cm3] }
{ Interpolated library name }
e.g, mox14x14
Initial Pu wt %
1 irradiation period per cycle
1 power (MW/MTU) per cycle
e.g., “mox_interpolated.f33”
Initial fissile Pu fraction (% 239Pu/Pu)

## Slide 37: ARP input example (MOX)
mox_w17x17
6.65
58.5
1
3
400 400 350
40 35 30
1 1 1
0.732
mox_interpolated.f33
Westinghouse 17x17 lattice with MOX fuel
6.65% initial Pu wt %
3 irradiation cycles
40, 35, & 30 MW/MTU
Interpolated library name
400, 400, & 350 day cycles
1 library per cycle
0.732 g/cm3 mod. density
58.5% fissile Pu fraction
Dummy entry

## Slide 38: Your turn: MOX fuel calculations with Origen
Calculate the plutonium isotopic composition from your last LEU case, decayed to 10 years
  i.e., output by weight % in Fulcrum for Pu
Using the same irradiation history as your 3-cycle LEU input, calculate the discharge isotopics & decay heat for 1 MTU of MOX
  Use a mox_w17x17 lattice
  Assume 1 MTHM fuel with 6.5% Pu & a balance of 0.25% enriched U tails

## Slide 39: Decay heat comparison
How does the decay heat per MTHM (in watts) from MOX compare to LEU:
  At 10 years?
  At 100 years?
  At 1000 years?

## Slide 40: Separations / reprocessing in Origen
Origen can separate out streams (by element) from a depletion case using the processing block
Atom fractions specified in the retained array are kept; all others become zero within the stream
case(PUREX){
…
processing{
% Structure: element=frac
% i.e., keep 50 a/o U and 99 a/o Pu
retained=[ u=0.50 pu=0.99 ]
}
}

## Slide 41: Continuous removal of elements in processing
Origen can also handle continuous removal of elements (e.g., off-gas handling, continuous feed/removal) in the processing block
Multiple removal rates (covering groups of elements) can be specified
case(off_gas){
…
processing{
% Removal rate in 1/s
removal{ rate=1e-2 ele=[H Xe Ar] }
removal{ rate=1E-7 ele=[U Pu] }
}
}
Notes: Continuous removal effectively acts like an artificial increase in the decay constant

## Slide 42: Stream blending from multiple cases
Origen can combine streams from named cases into a combined stream
  Useful for waste & recycle calculations
Caveat: Only one blend keyword may appear in the entire Origen input
  i.e., between origen= & end

## Slide 43: Blending case example
case(rad){
% Irradiation happens here
…
}
case(waste){
…
% process irradiated fuel;
% keep just FPs
processing{
retained=[ pu=0.99 ]
}
}
case(blend_glass){
% Vitrified HLW
mat{
% Use 10% of waste stream
% and 10% of glass stream
blend[waste=0.1 glass=0.1]
}
time={…}
…
}
case(glass){
% Borosilicate glass
mat{
units=GRAMS
iso=[li=2.18e3 b=2.11e3 o=46.4e3 f=0.061e3 na=7.65e3 mg=0.49e3 al=2.18e3
si=25.4e3 cl=0.049e3 ca=1.08e3 mn=1.83e3 fe=8.61e3 ni=0.70e3 zr=0.88e3
pb=0.049e3]
}
time{ t=1 start=0 }
}
2
1
3